I

The structure had a General Inspection in June

no concerning issues were found. Please see the inspection results below;

| Defect XSP Start End | Parameterl Value | Parameter 2 L.XCode Description Value |
| --- | --- | --- |
| BI01 | 0 | 01- | No Defect | A No d efect | restricted access, see comments |  |
| BIOS | 0 | 01- | No Defect | A No defect | restricted access, see Nol |  |
| BI06 | 0 | 02- | Minor | BSIighKSSS | 2.2 - Reinforced Concrete, Prestressed Concrete and Filler Joist - Minor localised spalls exposing shear links |
| BIOS | 0 | 0 | 1- | No Defect | A No defect |  |  |
| BI09 | 0 | 0 | 1- | No Defect | A No defect | restricted access, see Nol |  |
| BI16 | 0 | 0 | 1- | No Defect | A No defect | restricted access, see Nol |  |
| BI17 | 0 | 0 | 1- | No Defect | A No defect | restricted access, see Nol |  |
| BI21 | 0 | 0 | 3- | Moderate | CM ode rate 5-20% | 4.1 - Paintwork and Protective Coatings - Spot, chips and cracks of finishing coat, undercoat sound plus localised failure, see No23 | exposed but |
| BI23 | 0 | 0 | 2- | Minor | BSIight<5% | 2.2 - Reinforced Concrete, Prestressed Concrete and Filler Joist - Minor localised spalls exposing shear links |
| BI23 | 0 | 0 | 3- | Moderate | B Slight <5% | 2.3 - Reinforced Concrete, Prestressed Concrete and Filler Joist - Cracks and crazing in areas Cracks approx. 1mm and easily visible to safety fenceing post SE | of high flexure. |
| BI23 | 0 | 0 | 2- | Minor | B Slight <5% | 1.1 - Metalwork - Minor surface rusting |  |
| BI23 | 0 | 0 | 2- | Minor | B Slight <5% | 13.1 - Impact Damage - Slight impact deformation of steelwork infill E |  |
| BI23 | 0 | 0 | 5- | Failed | BSIight<5% | Missing top rail to concretev safety fencing atop bank SW and broken post atop bank SW, if | relevant? |
| BI24 | 0 | 0 | 2- | Minor | B Slight <5% | 9.4 - Surfacing - Cracks in top layer |  |
| BI25 | 0 | 0 | 2- | Minor | B Slight <5% | 9.2 - Surfacing - Minor crazing, tracking and/or fretting |  |
| BI25 | 0 | 0 | 2- | Minor | B Slight <5% | 5.1 - Vegetation - Minor vegetation causing no structural damage (surface mosses, small grass and weeds) |
| BI25 | 0 | 0 | 2- | Minor | B Slight <5% | 9.4 - Surfacing - Cracks in top layer |  |
| BI26 | 0 | 0 | 1- | No Defect | A No defect |  |  |
| BI31 | 0 | 0 | 2- | Minor | B Slight <5% | Minor separating cracking at construction joints to all wingwalls |  |
| BI31 | 0 | 0 | 2- | Minor | B Slight <5% | 3.7 - Masonry, Brickwork and Mass Concrete - Minor displacement to all wingwalls at joints to abutments |
| BI33 | 0 | 0 | 3- | Moderate | B Slight <5% | 5.2 - Vegetation - Significant depth/density of vegetation, obscuring inspection to bank NW | only |
| BI35 | 0 | 0 | 1- | No Defect |  | None provided |  |
| BI90 | 0 | 0 |  |  |  | boat required to view underside of structure ^L |  |